PRODUCT INFORMATION

NYLO-PRINT

## Main Characteristics

| Finish | Drying | Thinner Wash up | Mesh | Stencil | Coverage | Application | Colour Range |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Gloss | Not suitable for jet drying. Touch dry approx 1 to 2 hours, full cure 7 days. | Thinner NP 180 Retarder NP 182 Wash Up SU5112. | Mono Filament fabric 43t to 62t. | Any non solvent based emulsion. | Approx 40 sq mt per kg. | Refer to A.S.I ink selector chart. | 8 Standard plus Black and White. Not available in Basic Pantone. |

PRODUCT DESCRIPTION:

Nylo-Print inks are a flexible and elastic ink suitable for printing on most synthetic and natural fabrics.  The system has displayed a high degree of resistance to laundering and dry-cleaning.

The Nylo-Print series is a two pack system that dries by polymerisation. Nylo-Print catalyst NP176* is mixed in a ratio of 3 parts catalyst to 7 parts Nylo-Print ink prior to printing, this addition initiates the polymerisation (curing) process. The system will NOT fully cure without the addition of catalyst.

Prints will air dry in approximately 30 minutes with full resistance properties developed after 7 days. As an alternative, and if the printed substrate will withstand it the prints may be forced cured 93 Deg.C (250.F) for approximately 7 to 10 minutes.

* Catalyst NP176 is moisture sensitive and should be stored in a dry place.

Substrate and End-Use:

Acceptable results have been achieved with this ink on waterproof nylon, nylon/polyester blends and sailcloth, however due to the wide batch variation in this range of materials all substrates must be print checked on a batch by batch basis.

Thinners

Thin up to 15% with Nylo-Print Thinner NP180. To retard drying thin with Nylo-Print Retarder NP182.

Opacity and Lightfastness:

| Number | Description | Opacity | Lightfastness | Number | Description | Opacity | Lightfastness |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 111 | Black | Opaque | Excellent | 32 | Lemon Yellow* | Semi Opaque | Good |
| 112 | White | Opaque | Excellent | 52 | Golden Yellow* | Semi Opaque | Excellent |
| 22 | Fire Red* | Semi Opaque | Good | 42 | Emerald Green* | Opaque | Good |
| 24 | Orange* | Semi Opaque | Good | 52 | Light Blue | Opaque | Excellent |
| 30 | Primrose Yellow* | Opaque | Good | 57 | Royal Blue | Opaque | Excellent |

* Also available in excellent lightfast, fully opaque lead pigment form.

General Remarks:

Stir well before use. Always test apply ink before starting production run as there is often considerable difference between like substrates from different suppliers.

It is recommended that the Nylo-Print, M.S.D.S be consulted before using this product.